## Slide 1
08/19/2022
At 10 K, check alignment. Using the imaging system, put the beam spot in the circle and then align the sample to the mark on the screen.
Cool down to 10 K from 150 K (the initial plan was to do fine step measurements from 10 K to 50 K to verify the phase transition from 6 lobes to 4 lobes)
Check SHG signal in a single scan. With EM gain 300, see very strong signal in 1s.
Take a full circle of SHG scan, using EM gain = 300, exposure = 1s, accumulation = 2. The SHG pattern clearly has 4 lobes.
Double check Chunli’s 10 K from 08/18/22. The exposure time was too high. As a result, the camera was over saturated.
Change plan: take 10 K step warm up measurements using EM 300, exp 1s and acc 2 setting. To warm up slowly, increase the temperature every 5K.
At 50 K, the rotary encode of the polarizer is off by 20 deg. Fix it.
Check alignment at 40 K and 80 K, the thermal drift is less than 10 micron.